| Self Laminating Clear Polyvinylidene Fluoride Film |
| --- |
| This specification is intended to outline the physical and chemical properties of Panduit’s pressure sensitive self laminating polyvinylidene fluoride material and include the following part numbers and printable material identifiers: |
| Part Number Prefixes |  | Printable Material Suffixes |
|  |  |  |  | T1T |  |  |
|  |  |  |  | T1J |  |  |
|  |  |  |  | T1D |  |  |
| PRODUCT SPECIFICATIONS: |
| Description: | Material is RoHS compliant (European Union directive 2002/95/EC). Material is a self-extinguishing top coated polyvinylidene fluoride film with a pressure sensitive adhesive. This material is intended for interior and exterior markings and used in a self-laminating format for wire/cable marking. |
| Print Methods: | This material is recommended for dot matrix, thermal transfer, laser and inkjet printing. |
| Adhesive: | Acrylic based, pressure sensitive permanent adhesive. |
| Standard Colors: | Clear film with white print-on area |
| Thickness: | 1.8 +/- 0.3 mils (substrate and adhesive) |
| Service Temperature Range: | -650F to 2750F(-53.90C to 1350C) |
| Minimum Application Temperature: | 50°F (10°C) |
| Storage Conditions: | Store at 70°F (21°C) and 50% Relative Humidity. |
| PROPERTIES: | PERFORMANCE: |
| Peel Adhesion to Stainless Steel: | 30 oz/in width (PSTC-1, 15 min. dwell) 66 oz/in width(PSTC-1, 72 hours dwell) |
| Shear Adhesion: | 24+ hours (PSTC-7, Procedure A) |
| Tensile Strength: | MD 7 lbs/inch +/-0.7 lbs/inch (PSTC-31) TD 7 lbs/inch +/-0.7 lbs/inch (PSTC-31) |
| Elongation: | MD 400% +/- 10% (PSTC-31) TD 125% +/- 10% (PSTC-31) |
| UV Resistance: | 3000 hours no change observed (ASTM G151) |
| Elevated Temperature Exposure: | After 24 hours at 160°F (70°C) there was no deterioration of the substrate |
| CHEMICAL/SOLVENT RESISTANCE: Samples were dot matrix printed with Panduit PDLR ribbon, thermal transfer printed with RMH4BL and RMW4BL ribbons, laser and inkjet printed. These samples were wrapped around a 1/12” OD wire in self-laminating format. Test was conducted at room temperature after 24 hour dwell. The samples were immersed in the specified chemical reagents for 5 immersions using the following cycle: a 10 minute immersion time followed by a 30 minute recovery time. Visual Observation Chemical Reagent Substrate / Adhesive Dot Matrix Printed Legend Thermal Transfer Printed Legend Laser Printed Legend Inkjet Printed Legend Distilled Water No effect No effect No effect No effect No effect Mineral Spirits No effect No effect No effect No effect No effect ASTM #3 Oil No effect No effect No effect No effect No effect Isopropyl Alcohol No effect No effect No effect No effect No effect Methanol Slight adhesive bleed No effect No effect No effect No effect 3% Alconox Detergent No effect No effect No effect No effect No effect 10% Sodium Hydroxide Solution No effect No effect No effect No effect No effect 10% Sulfuric Acid Solution No effect No effect No effect No effect No effect 5% Sodium Chloride Solution No effect No effect No effect No effect No effect Freon TF No effect No effect No effect No effect No effect Super Agitene No effect No effect No effect No effect No effect Jet-A Fuel No effect No effect No effect No effect No effect Arco TruSlide 68 No effect No effect No effect No effect No effect SAE 30 Motor Oil No effect No effect No effect No effect No effect |

# Text boxes

LIMITED WARRANTY

All Panduit Identification Solution Products (except for Software programs) are warranted to be free from defects in material and workmanship at the time of sale but our obligation under this warranty is limited to replacement of the product proved to be defective within 6 months from the date of sale, or in the case of printers, within 90 days from the date of sale.  This warranty is void if the products or printers are modified, altered or misused in any way.  Use of Panduit printers with any product other than the specified Panduit products for which the printer was designed constitutes misuse.  Before using, the user shall determine the suitability of the product for its intended use and user assumes all risk and liability whatsoever in connection therewith.  The foregoing may not be altered except by an agreement signed by officers or seller and manufacturer.

NEITHER Panduit OR SELLER SHALL BE LIABLE FOR ANY OTHER INJURY, LOSS OR DAMAGE, WHETHER DIRECT OR CONSEQUENTIAL, ARISING OUT OF THE USE OF, OR THE INABILITY TO USE THE PRODUCT OR THE PRINTER.

THIS WARRANTY IS MADE IN LIEU OF AND EXCLUDES ALL OTHER WARRANTIES, EXPRESS OR IMPLIED.  THE IMPLIED WARRANTIES OF MERCHANTABILITY AND FITNESS OF PARTICULAR USE ARE SPECIFICALLY EXCLUDED.

The information contained in this literature is based on our experience to date and is believed to be reliable. It is intended as a guide or use by persons having technical skill at their own discretion and risk. We do not guarantee favorable results or assume any liability in connection with its use. Dimensions contained herein are for reference purposes only.  This publication is not to be taken as a license to operate under, or a recommendation to infringe any existing patents. This supersedes and voids all previous literature, etc.